## Slide 1
Simulación de propiedades
Miriam Marqués Arias
Notes: 1
1

## Slide 2
Estructura Propiedades

## Slide 3
Intervalo de presión en el universo

## Slide 4
Un nuevo mundo bajo presión
Líquidos sorprendentes sólidos, gases metales exóticos…….. por modificación de distancias interatómicas y ángulos de enlace.
Transiciones de fase a nuevas estructuras cristalinas con propiedades físicas y químicas inesperadas y novedosas
Elementos se convierten en superconductores, metales se convierten en aislantes
Las moléculas se rompen
Nuevas reacciones químicas son posibles (hidruros de elementos de transición)

## Slide 5
Transiciones de fase

## Slide 6
Una nueva tabla periódica

## Slide 7
Na: fase hP4
hP4 : aislante con band gap directo (Eg=2.1 eV)
Cuencas de ELF: unidades localizadas sin conexión. Puede esto ayudarnos a entender la conductividad?
(W. Kohn, Phys Rev A 133,171: Theory of the insulating state”)
Qué es un metal?

## Slide 8
Simulación computacional?
EXPERIMENTO:
“Invisible”
System
INPUT
ESTÍMULO
OUTPUT
RESPUESTA
MODELO:
Descripción simplificada de un sistema real y complejo
Captura la física esencial responsable del comportamiento del sistema
Obvia los detalles irrelevantes sin impacto significativo en la respuesta
El resultado del modelo tiene que estar de acuerdo con los experimentos, si no puede ser demasiado simple
Los modelos permiten extrapolar la respuesta del sistema en condiciones no accesibles por los experimentos

## Slide 9
Simulación computacional?
MODELO:

## Slide 10
Simulación computacional?
MODELO:
Distancias, direcciones?
Conectividad O.K.
Qué nos interesa?

## Slide 11
Simulación computacional?
Experimentos
Teoría
SIMULACIONES
COMPUTACIONALES
Presentes en nuestra vida diaria (simulaciones en economía, previsión metereológica, simuladores de vuelos…)
Método general para resolver modelos que no pueden resolverse analíticamente por su complejidad
Se basan en algoritmos (series de instrucciones)

## Slide 12
Simulación computacional?
Experimento computacional: el ordenador sirve para resolver numéricamente las ecuaciones definidas por el modelo
Permiten testear diferentes modelos
Necesitamos herramientas para el análisis de los resultados de la simulación
En materiales: estudian el modo en que los componentes del sistema interaccionan entre ellos, con el entorno y frente a factores externos (presión, temperatura)
Modelo: ecuaciones que gobiernan el comportamiento
Simulación: resultado del modelo con cierta precisión
Experimento: medida de propiedades con cierta precisión

## Slide 13
PROPERTIES
electronic
magnetic
vibrational
optical
Goal: Describe properties of matter from theoretical methods firmly rooted in fundamental equations
sstructural

## Slide 14
EXPERIMENTS
+ characterization
techniques
PROBLEMS:
Small size of the sample
No hydrostaticity
Limited range of pressures
Non recoverable structures
Lack of crystallinity
Pressure sensors
Transition mechanisms
SIMULATIONS
ideal samples
any conditions
It allows:
Complement experiments
Interpret and predict
PROBLEMS:
approximations
experiment-theory comparison

## Slide 15
Ab initio simulations

## Slide 16
Density functional theory

## Slide 17
In a crystal?

## Slide 18
Periodic crystals

## Slide 19
Periodic crystals

## Slide 20
Periodic crystals

## Slide 21
Calcite: fluorite structure

## Slide 22
Primitive cell

## Slide 23
Basis sets: Plane waves

## Slide 24
Brillouin zones

## Slide 25
Cutoff: finite basis set

## Slide 26
Advantages of plane waves

## Slide 27
Pseudopotentials

## Slide 28
Pseudopotentials

## Slide 29
Pseudopotentials

## Slide 30
Brillouin zone integration

## Slide 31
Brillouin zone integration

## Slide 32
Monkhorst-Pack grid

## Slide 33
Integrations in the IBZ

## Slide 34
Smearing methods

## Slide 35
Electronic structure codes

## Slide 36
Total energy & derivatives

## Slide 37
Total energy & derivatives

## Slide 38
Structure searching
“One of the continuing scandals in the physical sciences is that it remains in general impossible to predict the structure of even the simplest crystalline solids from a knowledge of their chemical composition” (Maddox, Nature 1988)
What structure will a collection of atoms adopt?

## Slide 39
Potential energy surfaces
Crystal structure prediction: minimization of Gibbs free energy
G= U + pV –TS. Normally, H= U +pV is minimized.
d= 3N+3 (N= number of atoms).

## Slide 40
Potential energy surface = a fractal?
A big region of the PES contains almost no minima: it corresponds to very high-energy structures with unphysical short distances and fragmented units.
Going from one minimum to another minimum of lower energy is more likely when the barrier between basins is small.
Basins with lower-energy minima tend to have larger hyper-areas than higher-energy minima.
Very low-energy minima usually correspond to symmetrical structures.

## Slide 41
Semilocal methods
They need a good initial starting guess.
Exploration on the neighbourhood of this low-energy
structure and subsequently found structures.
Simulated annealing
Minima hopping
Basin hopping
Metadynamics

## Slide 42
Simulated annealing
Mimics the metallurgy process to reduce defects & obtain large single crystals. Heating & cooling in a controled way.
When a metal melts, atoms in a disorded state in which atomic diffusion and kinetic barriers crossing are allowed.
An abrupt decrease of T leads to crystals with defects.
But ,if cooling is slow, atoms arrange in the global minimum.

## Slide 43
Simulated annealing
A candidate structure is continuosly perturbed through random atomic displacements, atomic mutations, changes of lattice parameters using a Monte Carlo scheme.

## Slide 44
Simulated annealing
Move accepted if, Ef< Ei or ε < P, P=exp(-ΔE/KBT).
Simulation starts at high T (most of new configurations accepted, kinetic barriers overcomed easily).
Then, temperature is reduced, fewer high-energy configurations accepted….an hopefully, the global minimum will be found.
PROBLEMS:
system stuck in a local minimum or the wrong funnel……. especially if there are surrounded by high energy barriers.
EFFICIENCY depends strongly on:
Type & magnitude of moves. Large enough to jump local minima, but small to enable learning.
Temperature annealing process.

## Slide 45
Basin hopping
It starts at a random configuration, relaxed to its local minimum.
After a random move, the new configuration is also relaxed to its local minimum.

## Slide 46
Basin hopping
Metropolis criterion, Ef< Ei or ε < P, P=exp(-ΔE/KBT) on the minimized energies.
Temperature can be maintained or constantly reduced.
Original PES transforms into a staircase function representing the energies of the local minima.
Barriers between local minima are smaller and jumping easier.
EFFICIENCY depends strongly on:
Type & magnitude of moves.
Choice of temperature.

## Slide 47
Minima hopping
It uses molecular dynamics to overcome barriers.
It starts at a local minimum. The MD simulation is stopped when U reaches another minimum.

## Slide 48
Minima hopping
START from a local minimum “Min”
ESCAPE TRIAL
Molecular dynamics+ Relaxation to “M”
Check if escaped from “Min”
REJECT NEW MINIMUM
Ediff=Ediff*2
(2 >1)
ACCEPT NEW MINIMUM
“Min” = “M”
Ediff=Ediff*1
(1 <1)
If E(“M”)-E(“Min”) < Ediff
FALSE
TRUE

## Slide 49
Minima hopping
It exploits the Bell-Evans-Polayani principle, it moves from one minimum to another by crossing low barriers which significantly increases the probability of hopping into a low energy local minimum.
Exothermic reactions have a low activation energy.
Reactant and product are neighboring minima and chemical reactions are transition of barriers connecting them.
Low Ekin in MD for hops into low neighboring minima

## Slide 50
Minima hopping
Inner Loop
Perform MD escape trials followed by local geometry relaxation.
Ekin continuously adjusted.
Outer Loop
Accepting or rejecting. Dynamic Ediff: 50 % accepted
Eventually accept high energy structures.
EFFICIENCY depends on Ekin.
Too high visiting lots of undesirable minima
Too low big number of MD simulations to escape the current basin of attraction

## Slide 51
Metadynamics
Ideally, standard NPT MD simulations allow to simulate phase transitions (structure prediction & kinetics).
But, they face a time scale problem, only transitions with activation barriers < kBT are observable with reasonable ts.
Solid-solid phase transitions generally first-order high barriers & slow.
Periodic boundary conditions NO heterogenous nucleation; transition proceeds in a collective & concerted way with large barrier.
It can lead to unrealistic kinetics & skipping of phases.

## Slide 52
Metadynamics
Solution to decrease barrier: adding a suitable potential to the original Gibbs energy landscape.
Search for the lowest-energy path connecting 2 minima in the space of a suitable order parameter (supercell box m.).

## Slide 53
Metadynamics
G modified by a history-dependent term: sum of Gaussians placed at visited points to discourage dynamics from visiting them again.
Basin of atraction filled with Gaussians that increase G. When G becomes high enough to overcome the barrier, the system enters a new basin of atraction of a new structure.
EFFICIENCY depends on:
Width & amplitude of Gaussians.
Too large may lead to wrong phase transitions
But too small, may require too many metadynamics steps.

## Slide 54
Global methods
They do not need a good initial starting guess.
Initial randomly generated structures
Random structure searches
Evolutionary algorithms
Particle swarm optimization technique

## Slide 55
Random searching (AIRSS)
The simplest approach if nothing is known about the system
Exploration of the whole PES by calculating the Gibbs free energy of a set of random structures.

## Slide 56
Structure searching (AIRSS)
input: pressure, volume, number of atoms
Make a random unit cell
Throw a given number of atoms, of given type into the unit cell
Relax carefully under quantum-mechanical forces and stress
Repeat
Look for the lowest energy or more “interesting” structures
The recipe

## Slide 57
Structure searching (AIRSS)
Example: Silicon

## Slide 58
Structure searching (AIRSS)
Problem: Exponential wall
The number of metastable states is expected to increase exponentially with the system size
Solution: Use of constraints
Based on: chemical ideas, symmetry, experimental data.

## Slide 59
Evolutionary algorithms
Inspired by natural evolution of a population where offspring resemble parents & procreation is a reward for success.
Different computational codes: XtalOpt, GASP, USPEX….
Initial (random) population of structures. Constraints: estimated volume, minima ds, symmetry, lattice parameters, seeding with plausible structure, using building blocks…..
After relaxing structures, a fingerprint & fitness are assigned to each structure.
Identical structures are eliminated to prevent cancer growth.
Select lowest-energy structures as parents for new generation.
Standard variation operators: heredity, lattice mutation, permutation, atomic mutations.
The best structure survives into the next generation & random structures also added to preserve diversity.

## Slide 60
Evolutionary algorithms
Procedure repeated until lowest E structure does not change.

## Slide 61
Particle swarm optimization
Swarm intelligence: information exchanges between individual particles, self-improving evolution, evolution guided by optimal particle.

## Slide 62
Particle swarm optimization
Similar to evolutionary methods, but no evolution operators such as heredity or mutation.
First population (swarm) randomly generated with constraints.
Local optimization & discarding of identical structures.
A fraction of the lowest E structures used to produce 60% of the structures in the new generation. (40% random).
Movement of the particles influenced by their individual past experience (pbestt, vt) and that of the swarm (gbestt).
As the evolutionary methods, it learns from history and zooms in the most promising region of the configurational space.

## Slide 63
Particle swarm optimization
Algorithm

## Slide 64
Particle swarm optimization
Algorithm

## Slide 65
Convex hull and stability

## Slide 66
Convex hull and stability
2D 3D
H2, S, Se, H2S (H:2/3,Se:0, Se:1/3) estables
Phase diagrams in Materials Project, choice of: elements, máximum energy above hull, exchange-correlation…..at 0 GPa

## Slide 67
Convex hull and stability
AIAIRSS calculations
100, 300, 700 Ga
400.000 structures
HCNO: stable
regla del octeto
Isoelectrónicos a diamante
Deficientes en hidrógeno
L. J. Conway PNAS 2021

## Slide 68
Reconciliation of chemistry and quantum chemistry
Quantum Chem.
System:Global
Concepts: rigorous,
quantitative
Classical Chem.
System:Atoms, Bonds
Concepts: empirical,
qualitative
ELF
Mathematical definition of bond
Quantitative bond properties (q,v)
The Electron Localization Function

## Slide 69
In an attempt to better understand electron localization from a theoretical standpoint, Becke and Edgecombe developed in 1990 the electron localization function (ELF).
It can be interpreted in terms of an excess of local kinetic energy due to the Pauli repulsion.
Pauli
repulsion
The Electron Localization Function
Notes: 69
69

## Slide 70
What does it look like?
  ELF is maximal in Lewis entities
  Bonds
  Lone pairs
  Shells
LiCl
K(Cl)
L(Cl)
M(Cl)
The Electron Localization Function
Notes: 70
70

## Slide 71
Each bond, lone pair=maximum of ELF
Each maximum has an associated region of space (basin)
  Non overlapping
  They fill up the volume
Each region has its own properties, which
  are additive
  recover the crystal value
  E.g. volume, charge associated to a bond.
Number, position and type of critical points (maxima, minima,etc) determine the topological features.
The saddle point that connects two basins is called the Bond Interaction Point (bip).
The Electron Localization Function
Notes: 71
71

## Slide 72
Alkali metals at HP
It is becoming strikingly clear that the free-electron model of simple metals is not applicable when metals are compressed at intermediate pressures.
New structures appear: open, incommensurate structures
Unusual properties: decreased conductivity and melting points, superconductivity
This challenging state of matter has been explained in terms of FSBZ interactions, s→p or s→d electronic transitions, and more recently related to an increase of valence electron density in interstitial regions.
Notes: 72
72

## Slide 73
Alkali metals: structural transformations under pressure
Notes: 73
73

## Slide 74
K: hP4 phase
Crystal structure: hexagonal, SG P63/mmc, two different sites (Wyckoff 2a (0,0,0) and 2c (1/3,2/3,1/4))
c/a=3.266
c/a=1.36

## Slide 75
K: hP4 phase
Localization regions in interstitial voids
Core-like topology
Same structure as A2X compounds!
Electrons in same position as anions!
Close packing preserved if are considered!
ELF=0.3
ELF=0.9
Experimental potassium at P=27 GPa
COMPOUND→IONIC-LIKE
ELECTRONS→PSEUDOANIONS

## Slide 76
K at 58 GPa?
tI4 structure predicted by variable-cell simulations
behaviour of alkali-metal chalcogenides?
cation sublattice of anticotunnite structure:
SG: Pnma, Pearson oP8, K1 and K2 atoms locate on 4c sites .
subgroup of the Ni2In-type structure

## Slide 77
K: oP8 phase
Similar calculated oP8 and experimental diffraction pattern. Excellent Rietveld refinement.

## Slide 78
K: electride phases
25 GPa
(ELF ≈ 0.95)
Same structure as A2X (Ni2In)
57 GPa
(ELF ≈ 0.95)
Same structure as A2X (anticotunnite)
hP4 phase of K.
K→Alkali chalcogenide
oP8 phase of K.
Chalcogenide
position
Chalcogenide
position

## Slide 79
K: origin of phase transitions
DRIVING FORCE OF DISTORTIONS AT INTERMEDIATE PRESSURES? GREATER LOCALIZATION
25 GPa: phase transition towards strong interstitial localization (ELF=0.95)
25 GPa. If no transition took place, localization would be a lot weaker
c/a collapse
3.2→1.35
10 GPa: Normal metal.

## Slide 80
K: origin of phase transitions
57 GPa: Elongated basins appear showing a flow of electronic localization towards other sites and instability of the phase vs distortion
57 GPa with oP8 distortion. Distorted phase favors strong localization (ELF value close to 0.95)
oP8 distortion

## Slide 81
K at higher pressures?
Above 85 GPa, the electronic flow completes, metallic ELF maxima.
Predicted transitions to tI4 and oC16 structures.
Recovery of the dhcp arrangement above 250 GPa.

## Slide 82
Li at high pressures
Our experiments:
x-ray diffraction studies (P= 5-130 GPa, T=77-300K)
  Extremely difficult: chemical reaction/Li penetration into diamonds
cI16 60 GPa Li-VI 65 GPa Li-VII 95 GPa Li-VIII
Structures of Li-VI, Li-VII and Li-VIII (first time observed)?
  Proposed as oC88, oC40 and oC24.
After refinement:
oC24 has the Cmca-24 structure proposed previously.
oC40: cell parameters and Cmca space group
oC88: cell parameters and Cmma space group. oC92?

## Slide 83
oC40 Li
Our calculations:
AIRSS approach (random structure searching + DFT calculations)
CASTEP code, PBE PP, cutoff energy: 350 eV……..
Stringent reoptimization of the lowest-enthalpy structures
oC40 structure:
20-atom primitive cells, initial expt. lattice parameters
Using the experimental symmetry as a constraint
Searches within P21/c (subgroup of Cmca), Pc, randomly-selected space groups with 4 and 2 symmetry operations and no symmetry (P1).

## Slide 84
oC40 Li
C2cb-40 struct. is a subgroup of Cmca-40 struct.
P21/c
Cmca-40
Pc
4 symm. ops.
2 symm. ops.
P1
C2cb-40
Initial structures
Lowest enthalpy structure

## Slide 85
oC40 Li
From H-P curves:
C2cb-40 is the most stable phase between 67-90.5 GPa.
Hypothetically:
C2cb-4091GPa Cmca-24
C2cb-40 90.5 GPa Pbca-24 94 GPa C2cb-24 110GPa Cmca-24

## Slide 86
Dynamical stability?
Phonon calculations with the Quantum-ESPRESSO code.
Imaginary frequency for a B3u mode of the Cmca-40 struct.
Phonon dispersion curves of the C2cb-40 structure: dynamically stable
oC40 Li

## Slide 87
oC40 Li
Semiconductor?
Indirect band gap along ΓZ similar to the Γ-direct band gap
Gap increases with pressure, 1.15 eV at 95 GPa
Larger gap than the other structures (0.276 eV for the C2-24)

## Slide 88
oC40 Li
Modulated layers. 5 neq. Li atoms, 3 ELF attractors.
M1: 2 e-s, M2: 2 e-s, M3: 1e- Li5ABC.
New elemental structure, not found previously.

## Slide 89
oC88 Li
oC88 structure
44-atom primitive cells, initial expt. lattice parameters.
Searches within the P2/c, Pc, C2 space groups and randomly selected space groups with 2 symmetry ops.
Additional searches in oC92 and oC84 structures
Lowest enthalpy structure: C2mb space group.
More stable than the rest of the phases (except cI16) in its experimental range of existence
Stabilized by dynamical effects? Metastable?
Reasonable agreement with diffraction data

## Slide 90
oC88 Li
Complicated structure.
low DOS at EFERMI, but no band gap.

## Slide 91
Vibrational effects on Li
Very low frequency modes in oC88.
Intense and rich spectrum in oC40 and intense mode in oC24.
Raman

## Slide 92
Vibrational effects on Li
Gibbs free energies calculated using QHA approx.
G= U + PV + kBT∫g(ω)ln[2sinh(ħω/2kBT)]dω.

## Slide 93
Vibrational effects on Li
Neglecting ZPE at OK

## Slide 94
Vibrational effects on Li
With ZPE at OK

## Slide 95
Vibrational effects on Li
oC88 becomes stable at finite T

## Slide 96
Incommensurate structures
I
Common host structure
Tetragonal I4/mcm
16 atoms
Notes: 96
96

## Slide 97
Incommensurate structures
I
Different guest structures
Notes: 97
97

## Slide 98
Incommensurate structures
I
Different guest structures
Notes: 98
98

## Slide 99
Incommensurate structures
I
Different guest structures
Notes: 99
99

## Slide 100
Incommensurate structures
I
Different guest structures
Rb-IV: I4/mmm, 2a (0,0,0)
aguest = ahost
chost/guest= 1.631
Notes: 100
100

## Slide 101
Computational approach
I
cH/cG chosen to cover the respective experimental range
4g/3h (56 atoms), 3g/2h (38 atoms), 8g/5h (96 atoms), 5g/3h (58 atoms), 7g/4h (78 atoms), 9g/5h (98 atoms), 2g/1h (20 atoms)
Unit cells for K-IIIb are twice as large
cH/cG: 1.3333, 1.5, 1.6, 1.6666, 1.75, 1.8, 2
Na-V approximants with tetragonal guest lattices
Empty tI19 host lattice
3g/2h approx.
7g/4h approx ( )
Notes: 101
101

## Slide 102
Potassium
I
9
bcc fcc at 11 GPa
17.5 GPa < tI19 < 39 GPa
oP8 tI4 at 51 GPa
tI4 oC16 at 96 GPa
K-IIIa < 23 GPa
23 GPa < Rb-IV > 38 GPa
K-IIIa > 38 GPa
Notes: 102
102

## Slide 103
Potassium
I
9
Optimal cH/cG at each P
Parabollic fits H--cH/cG
Minimum cH/cG (24 GPa)
cH/cG = 1.5---1.66
Approximants with cH/cG from 1.5 (3g/2h structure) to 1.8 (9g/5h structure)
6-8 GPa offset calculated vs measured cH/cG curves
Notes: 103
103

## Slide 104
Na-V structure (ELF)
I
Guest ELF maxima
ELFav=0.94
HHost ELF maxima
ELFav=0.965
Guest ELF maxima
ELF(bip)=0.85
1.058 e-/max
0.02961 e-/bohr3
Host ELF maxima
ELF(bip)=0.35
1.695 e-/max
0.02994 e-/bohr3
At 160 GPa
Notes: 104
104

## Slide 105
K-IIIa (ELF)
I
Guest ELF maxima
ELFav=0.89
HHost ELF maxima
ELFav=0.95
Guest ELF maxima
ELF(bip)=0.49
0.721 e-/max
0.01826 e/bohr3
Host ELF maxima
ELF(bip)=0.15
1.165 e-/max
0.01680 e/bohr3
Notes: 105
105

## Slide 106
xSiO2 + yCO2 -> SixCyO2x+2y
18-26 GPa & 296-980 K

## Slide 107
After optimization…
Distorted CO4 + SiO6 units
unstable vs decomposition into CO2-III and SiO2-stishovite
Is there any SiCO compound?
From database analysis
Candidate structure UB2O6 & (C2/c, Z=4)
Correct Si1-xCxO2 stoichiometry & BO3 units

## Slide 108
Global SixCyO2(x+y) searches
Our calculations:
Searches with the USPEX code + DFT calculation
VASP code, PBE PP, cutoff energy: 600 eV...
Stringent reoptimization of the lowest-enthalpy structures
x,y =1-3; Z = 1-4. Selected pressures from 0 to 100 GPa
Initial population:
random + C(Si)O2-derived + CO4, SiO4, CO3, SiO6 units
Generations with 40Z structures (heredity & random)
Convergence reached on 30-60 generations.

## Slide 109
Global SixCyO2(x+y) searches
ΔH = H(SixCyO2(x+y)-xH(SiO2)-yH(CO2)
0 13 18.2 100
GPa
Pa-3 P42/mnm β-cristobalite
CO2
0 4.8 8.5 55 85 100
SiO2
α-quartz coesite stishovite CaCl2-type α-PbO2-type
ΔH < 0
Stable SixCyO2(x+y)

## Slide 110
Global SixCyO2(x+y) searches
On pressure increase,
Minima ΔH region in the experimental range of stability.
Lowest H structures consisting of SiO6 and CO3 units.
SiC2O6,
Thermodynamically stable
P21/c structure, Z=2

## Slide 111
1935
Superconducting hydrogen
1968
…
Metallic hydrogen
ICMCS Seminar
R. Howie et al. 2020
MolecularMol Insulating
Low pressure
Metallic
High temperature superconductor
High temperature Superconductor
H-H
rH−H​(H2​)≈0.74 Å
rH−H​ ≈0.9 -1-1.2 Å
High pressure

## Slide 112
R. Howie et al. 2020
All hydrides still require pressures 80-200 GPa for high Tc
Understand how Tc can be promoted whilst required pressure is decreased
1935
Superconducting
Hydrogen
1968
…
Metallic Hydrogen
…
Superconducting
Hydrides
2004
2015
Start of
“Hydride Era”
2026
The Field
Today
Notes: However, this is where hydrides come in
Almost 40 years later, the same neil Ashcroft proposed the idea of chemical precompression in hydrides
That is, that doping the hydrogen with a well selected element would exert chemical pressure on the hydrogen, reducing H-H distances, meaning the metallisation would be lowered AND the physical properties of metallic hydrogen would be preserved and able to be accessed in the lab!
And this really did open up the possibility of studying hydrogen-based superconductivity for researcvhers

## Slide 113
Fm-3m in theory symmetry breaks to R-3m
DFT predicted structures
CChemical pre-compression: Group 2 tetrahydrides
Quasi-molecular hydrogen units within octahedral interstices
H- in tetrahedra interstices

## Slide 114
La IA revoluciona la búsqueda de estructuras cristalinas
Nature (2023) · Google DeepMind – GNoME
“Scaling deep learning for materials discovery”
2,2 millones de nuevos compuestos predichos; 380.000 estables (~10× lo conocido).
Nature (2025) · Microsoft Research – MatterGen
“A generative model for inorganic materials design”
IA generativa que diseña estructuras con propiedades a medida.
Nature (2023) · A-Lab, Berkeley – Síntesis autónoma
“An autonomous laboratory for the accelerated synthesis of novel materials”
41 de 58 compuestos nuevos sintetizados en 17 días.
Más de 700 materiales de GNoME ya validados experimentalmente.
Estructuras cristalinas descubiertas (acumulado)
Eje Y: nº de estructuras · Eje X: periodo (cifras aproximadas)
≈48 mil
≈80 mil
≈300 mil
≈1 millón
2,2 millones
Pre-2010
ICSD exp.
2011–15
Materials Project
2016–20
OQMD / DFT
2021–22
OQMD 1M+
2023
GNoME
Fuentes: Merchant et al., Nature (2023) – GNoME; Szymanski et al., Nature (2023) – A-Lab; Zeni et al., Nature (2025) – MatterGen. Cifras del histograma aproximadas/acumuladas.

## Slide 115
¿Cómo funciona GNoME?
1. Generar candidatos
Sustituir en estructuras conocidas + composiciones nuevas
2. Red neuronal de grafos
Predice energía y estabilidad de cada candidato
3. Filtrar por estabilidad
Se conservan los cercanos a la convex hull
4. Verificar con DFT
Cálculo cuántico confirma los más prometedores
5. Resultado
2,2 M predichas · 380 k estables
Aprendizaje activo: los resultados de DFT reentrenan la red en cada ronda → eficiencia ~10×
¿Qué es una red neuronal de grafos (GNN)?
Cada cristal se representa como un grafo: los átomos son nodos y los enlaces, aristas.
Por “paso de mensajes” cada átomo aprende de su entorno y la red capta la geometría 3D.
Así predice la energía de formación en milisegundos, sin resolver la mecánica cuántica (DFT) en cada caso.
Claves del método
Solo los candidatos prometedores pasan a la costosa verificación con DFT.
Hallazgos: ~528 posibles conductores de litio y ~52.000 materiales en capas.
NaCl: grafo real (coordinación 6)
Cl
Cl
Cl
Cl
Cl
Cl
Na
cada Na ↔ 6 Cl (octaédrica)
Red neuronal asociada
E
entrada
capas ocultas
energía form.
NaCl (tipo sal de roca): cada Na⁺ se rodea de 6 Cl⁻. La GNN procesa el grafo y predice la energía de formación.
Fuente: Merchant et al., “Scaling deep learning for materials discovery”, Nature (2023). Esquema simplificado.

## Slide 116
¿Cómo funciona MatterGen?
1. Ruido inicial
Átomos, posiciones y celda generados al azar
2. Difusión inversa
Una red elimina el ruido paso a paso (denoising)
3. Generar cristal
Aparece una estructura nueva y ordenada
4. Guiar por propiedades
Ajuste fino: banda, módulo, magnetismo
5. Resultado
Material nuevo, estable y sintetizable
Generación condicional: en vez de cribar millones de candidatos, MatterGen diseña directamente materiales con las propiedades deseadas.
¿Qué es un modelo de difusión?
Parte de ruido aleatorio y aprende a revertirlo hasta formar un cristal coherente.
Genera a la vez los tipos de átomo, sus posiciones y los parámetros de red.
Con ajuste fino orienta la generación hacia una propiedad objetivo.
Claves del método
Generativo, no solo de cribado: crea estructuras desde cero.
Hallazgos: ~2× más probables de ser nuevas y estables y ~15× más cerca del mínimo de energía (DFT) que modelos previos.
Difusión: de ruido a cristal
ruido
intermedio
cristal
Red de difusión (denoiser)
x₀
entrada
capas ocultas
cristal limpio
La red de difusión revierte el ruido paso a paso hasta obtener un cristal ordenado (esquema simplificado).
Fuente: Zeni et al., “A generative model for inorganic materials design”, Nature (2025), Microsoft Research. Esquema simplificado.

## Slide 117
¿Cómo funcionan los potenciales efímeros (EDDP)?
1. Estructuras al azar
Se generan al azar muchas estructuras: átomos, posiciones y celda
2. DFT en una muestra
Calculamos con DFT la energía de unas pocas de ellas
3. Potencial efímero
Con esos datos entrenamos un potencial rápido, a medida del sistema
4. Relajar
Ese potencial relaja y descarta miles de estructuras a bajo coste
5. Validar e iterar
Confirmamos las mejores con DFT y reentrenamos el potencial
La idea clave: el potencial se entrena para una búsqueda concreta y luego se descarta, así se acelera la búsqueda aleatoria sin perder la fiabilidad del DFT.
¿Qué es un potencial efímero?
Es un potencial interatómico aprendido: estima la energía de una estructura mucho más rápido que el DFT.
Se entrena a medida para el sistema que estudias; no sirve como modelo general.
Como es tan barato de entrenar y usar, se crea para la búsqueda y luego se descarta (de ahí, “efímero”).
Claves del método
Combina dos ideas: la exploración al azar de AIRSS y la rapidez de un potencial aprendido, y así llega a sistemas más grandes.
Aprendizaje activo: se van alternando DFT y potencial, que mejora en cada vuelta.
Ciclo de búsqueda acelerada
Aleatorias
(AIRSS)
DFT
(muestra)
Potencial
efímero
Relajar
Aprendizaje activo: DFT ↔ potencial, se reentrena cada ciclo
Potencial efímero: ensemble de redes pequeñas
E
promedio
descriptores
3 redes pequeñas (ensemble)
energía
El potencial solo aprende energías; las fuerzas para relajar salen de derivarlo (esquema simplificado).
Fuente: C. J. Pickard, “Ephemeral data derived potentials for random structure search”, Phys. Rev. B 106, 014102 (2022). Esquema simplificado.

## Slide 118
Conclusiones
DFT calculations provide an accurate description of the structural and energetic properties of materials, serving as a reliable framework for assessing the stability of the predicted crystal phases.
Crystal structure prediction methods are effective tools for exploring the configurational space and identifying stable or metastable structures.
The combination of global structure search algorithms with DFT calculations is a powerful approach for materials Discovery.
Experimental-theoretical collaboration to interpret results, understand involved mechanism…..
Artificial intelligence is revolutionizing crystal structure prediction by accelerating the exploration of the configurational space, reducing computational costs.