## Slide 1: Grupo de Altas Presiones y Espectroscopía Universidad de Cantabria
Luis Gómez Fernández.

## Slide 2: Campus de la Universidad de Cantabria

## Slide 3: Infraestructura

## Slide 4: Infraestructura

## Slide 5: Infraestructura

## Slide 6: Infraestructura

## Slide 7: Infraestructura

## Slide 8: Infraestructura

## Slide 9: Infraestructura

## Slide 10: Infraestructura

## Slide 11: Infraestructura

## Slide 12: Infraestructura

## Slide 13: Líneas de investigación
PJT
PRESSURE

## Slide 14: ¡Muchas gracias!

## Slide 15: A₂CrX₄ Compounds
Different electronic transitions:
1. Charge-transfer (CT) transitions
e-
e-
e-

## Slide 16: A₂CrX₄ Compounds
Different electronic transitions:
2. d–d crystal-field transitions
Bernal et al., 2020, DOI: 10.48550/arXiv.2005.06212

## Slide 17: A₂CrX₄ Compounds
Different electronic transitions:
3. Spin-flip transitions
Kitzmann, W.R., Moll, J. & Heinze, K. Spin-flip luminescence. Photochem Photobiol Sci 21, 1309–1331 (2022). https://doi.org/10.1007/s43630-022-00186-3

## Slide 18: Why Cs₂CrCl₄?

## Slide 19: Study Objectives

## Slide 20: Study Objectives
1. Determine the pressure dependence of the optical absorption spectrum.

## Slide 21: Study Objectives
1. Determine the pressure dependence of the optical absorption spectrum.
2. Track Raman-active vibrational modes.

## Slide 22: Study Objectives
1. Determine the pressure dependence of the optical absorption spectrum.
2. Track Raman-active vibrational modes.
3. Measure the magnetic response.

## Slide 23: Experimental Setup

## Slide 24: Experimental Setup
Micro-crystal selection

## Slide 25: Experimental Setup
Micro-crystal selection

## Slide 26: Experimental Setup
Diamond Anvil Cell (DAC)

## Slide 27: Experimental Setup
Boehler Almax DAC
Diamond Anvil Cell (DAC)

## Slide 28: Experimental Setup
Boehler Almax DAC
Membrane DAC
Diamond Anvil Cell (DAC)

## Slide 29: Experimental Setup
Microspectrometer for optical absorption

## Slide 30: Experimental Setup
Microspectrometer for optical absorption

## Slide 31: Experimental Setup
Horiba T64000

## Slide 32: Experimental Setup
Horiba T64000

## Slide 33: Optical Spectrum at Ambient Conditions

## Slide 34: Optical Spectrum at Ambient Conditions

## Slide 35: Optical Spectrum at Ambient Conditions
1. d–d band with E1 = 1.25 eV and E2 = 1.40 eV

## Slide 36: Optical Spectrum at Ambient Conditions
d–d band with E1 = 1.25 eV and E2 = 1.40 eV
Spin-Flip with ESF1 = 2.32 eV and ESF2 = 1.97 eV

## Slide 37: Optical Spectrum at Ambient Conditions
d–d band with E1 = 1.25 eV and E2 = 1.40 eV
Spin-Flip with ESF1 = 2.32 eV and ESF2 = 1.97 eV
CT with ECT = 3.2 eV

## Slide 38: Optical Changes under Pressure

## Slide 39: Optical Changes under Pressure

## Slide 40: Optical Changes under Pressure

## Slide 41: Optical Changes under Pressure

## Slide 42: Raman Modes at Ambient Pressure

## Slide 43: Raman Modes at Ambient Pressure

## Slide 44: Raman Modes at Ambient Pressure

## Slide 45: Raman Modes at Ambient Pressure
Stretching modes: A1(D2h) 289, 278 , 232 and B1(D2h) 223 cm-1
Bending mode: A1(D2h) 200 cm-1
Wagging mode: B2+ B3(D2h) 161 cm-1

## Slide 46: Raman Modes at Ambient Pressure
Stretching modes: A1(D2h) 289, 278 , 232 and B1(D2h) 223 cm-1
Bending mode: A1(D2h) 200 cm-1
Wiggling mode: B2+ B3(D2h) 161 cm-1

## Slide 47: Raman Under Pressure

## Slide 48: Raman Under Pressure

## Slide 49: Raman Under Pressure

## Slide 50: Magnetic Behavior under Pressure

## Slide 51: Magnetic Behavior under Pressure

## Slide 52: Conclusions

## Slide 53: Conclusions
Electronic properties:
The behavior of the d–d bands under pressure indicates a reduction of the JT distortion under pressure.

## Slide 54: Conclusions
Electronic properties:
The behavior of the d–d bands under pressure indicates a reduction of the JT distortion under pressure.
The Spin-Flip transitions shift to lower energies. In terms of the Racah parameter B, they represent the increase of covalency effects.

## Slide 55: Conclusions
Electronic properties:
The behavior of the d–d bands under pressure indicates a reduction of the JT distortion under pressure.
The Spin-Flip transitions shift to lower energies. In terms of the Racah parameter B, they represent the increase of covalency effects.
The FWHM of the SF increases with pressure, likely a Fano resonance.

## Slide 56: Conclusions
Electronic properties:
The behavior of the d–d bands under pressure indicates a reduction of the JT distortion under pressure.
The Spin-Flip transitions shift to lower energies. In terms of the Racah parameter B, they represent the increase of covalency effects.
The FWHM of the SF increases with pressure, likely a Fano resonance.
The CT bands decrease under pressure, and anomalies are observed that may be due to structural transitions.

## Slide 57: Conclusions
Vibrational properties:

## Slide 58: Conclusions
Vibrational properties:
Raman peak intensity depends on crystallographic orientation consistent with polarization of vibrational modes.

## Slide 59: Conclusions
Vibrational properties:
Raman peak intensity depends on crystallographic orientation consistent with polarization of vibrational modes.
Comparison with isostructural Rb2CrCl4 identifies vibrational modes and polarizations.In (001)-oriented crystals:
  278 cm⁻¹ in-plane Cr–Cl stretching.
  200 cm⁻¹ in-plane Cr–Cl bending.
  Both influenced by antiferrodistortive structure.

## Slide 60: Conclusions
Vibrational properties:
Raman peak intensity depends on crystallographic orientation consistent with polarization of vibrational modes.
Comparison with isostructural Rb2CrCl4 identifies vibrational modes and polarizations.In (001)-oriented crystals:
  278 cm⁻¹ in-plane Cr–Cl stretching.
  200 cm⁻¹ in-plane Cr–Cl bending.
  Both influenced by antiferrodistortive structure.
Under pressure: All peaks blueshift, with mode-dependent coefficients. Largest shift: 278 cm⁻¹ (14 cm⁻¹/GPa). At least three structural phase transitions observed. JT-related modes persist across 0–25 GPa → JT distortion stable in all phases.

## Slide 61: Conclusions
Magnetic properties:
Tc rises with pressure up to 0.22 GPa, then drops (~5%), and increases again at 8.8 K/GPa linked to structural transition affecting canting angle.
Chemical vs applied pressure consistent: ΔTc ≈ 12 K (calc.) vs 9.2 K (exp.), in line with Cs2CrCl4 → Rb2CrCl4 trend.
Anomaly in Tc(P) (0.22 GPa) parallels d–d absorption intensity anomaly (0.54 GPa) → likely common origin.
Transition pressure shifts with temperature (0.22 GPa at 44 K → 0.54 GPa at 290 K), similar to K2CuF4; full phase diagram calculation required.

## Slide 62: Thank you for your attention!